## Slide 1: ME150 Materials Science and Engineering I
Prof. Dr. Sinan Kandemir
Department of Mechanical Engineering
2026 Spring Term, 3 Credits
Time:
Monday 13.30-15.15, Friday 14.30-15.15
Location: A01
MS Teams Code: ykm624l
Üniversiteye, Memlekete Özgürlük!

## Slide 2
INSTRUCTORS:
Sinan Kandemir
Room: Z16
E-mail: sinankandemir@iyte.edu.tr
Office hours: Monday 09.45-10.30
Teaching Assistants:
Büşra İrem Türkpençesi
Mehmet Yalçın Sırmalılar
Samedhan Yıldırım
Üniversiteye, Memlekete Özgürlük!

## Slide 3
COURSE MATERIAL:
  Lectures
  Required text book
  Materials Science and Engineering: An Introduction,
  William D. Callister and David G. Rethwisch, John
  Wiley and Sons Inc., It does not matter which edition
  you have!
  Website: http://www.wileyplus.com/college/callister
  Student Companion Site
        Users can manipulate molecules and crystals to better visualize atomic structure, Unit cells such as
        BCC, FCC, HCP, Crystallographic planes, directions,
        and defects, Polymer repeat units and molecules,
        Diffusion computations
Üniversiteye, Memlekete Özgürlük!

## Slide 4
OPTIONAL MATERIAL:
  Schaffer, J. P., Saxena, A., Antolovich, S. D., Senders, Jr., T. H. and Warner, S. B., “The Science and Design of Engineering Materials” R. D. Irwın, Inc.
  Shackelford, J. F. “Introduction to Materials Science for Engineers” Macmillan Publishing Inc.
Üniversiteye, Memlekete Özgürlük!

## Slide 5
Why do you need a lecturer if you have a book & HW assignments?
To explain the most difficult concepts of the chapter during the lectures
To provide you additional materials, which you cannot find in the book, but which could be very useful in your future research (please take notes)
To discuss and address any kind of questions and concerns on the course (during lectures, TA and office hours)
To use his/her experience in material science for any kind of consultations, which may be related to your current projects
To fairly grade your HW, Quizzes, Exams and etc., providing you the opportunity to get high final marks!!
  https://www3.nd.edu/~amoukasi/CBE30361/Lecture_1_2014_lecture.pdf
Üniversiteye, Memlekete Özgürlük!

## Slide 6
Suggestion for success in this lecture
Attendance is your job – come to class!
Read the relevant material in the book (preferably before the lecture!)
Review and understand the examples given in the book and/or website.
Do the assigned homework. If you are having difficulty with a particular concept, work additional problems given in the book and/or website on that topic that have the answers given in the back of the book.
Come to office and TA’s hours
Any suggestion/opinion/request are welcome
Academic success is directly proportional to the amount of time devoted to study!!
  https://www3.nd.edu/~amoukasi/CBE30361/Lecture_1_2014_lecture.pdf
Üniversiteye, Memlekete Özgürlük!

## Slide 7
ASSESSMENT:
Midterm: 35%
Quiz: 20%
Final exam: 45%
(Weighting may be slightly modified)
  Exams will be based on homework and information provided in lectures and assigned readings. All exams will be closed book. The final will be cumulative. Relevant formulas, tables, etc. will be provided.
  Please do not come to the office to ask additional points, etc.
Quizzes will be scheduled.
70% Attendance is required.
Final Exam score has to be higher than 40.
Üniversiteye, Memlekete Özgürlük!

## Slide 8
Several important issues
You should have a complete (100%) understanding of all concepts that I am talking about!!!
You should understand why this course is important!
Essentials
To share knowledge with passion
To be ready to help and support young engineers
To support creativity and willingness to learn
A high final grade for the student is my main goal
Let’s start
Üniversiteye, Memlekete Özgürlük!

## Slide 9
Course Objective...
Introduce fundamental concepts in Materials
Science
You will learn about:
• material structure
• how structure dictates properties
• how processing can change structure
This course will help you to:
• use materials properly
• realize new design opportunities
with materials
Üniversiteye, Memlekete Özgürlük!

## Slide 10
1. Introduction
What is materials science?
  Multidisciplinary field of science devoted to understanding and manipulating the different materials properties including physical, mechanical, electrical, etc. It investigates relationships that exist between the structure and properties of materials.
  Materials Engineering is on the basis of these structure-property correlations, designing or engineering the structure of a material to produce a pre-determined set of properties
Üniversiteye, Memlekete Özgürlük!

## Slide 11
Buehler and Ackbarow, Materials Today, 2007
Üniversiteye, Memlekete Özgürlük!

## Slide 12
Why should we know about it
  Mechanical engineering is among the most diversified of the traditional engineering disciplines. Mechanical engineers design and build machines and devices that enable humans to live and work in space, in the air, on the ground, and under water.
  Naturally, much of what engineers can or cannot do depends on the materials they have available to tackle their tasks. This is why engineers and material scientists work closely together with the goal of tailoring not only the mechanical, but also chemical and electrical properties of materials to make new applications possible.
  We have to be able to talk with materials scientist on the same professional language, formulate the problem and outline routes for it solution.
Üniversiteye, Memlekete Özgürlük!

## Slide 13
Üniversiteye, Memlekete Özgürlük!

## Slide 14
Understanding Materials
Processing → Structure → Properties → Performance
Optimization
Tetrahedron of Materials Science and Engineering
Material properties depend on the material micro/nano structure, which in turn, results from its composition and processing
Üniversiteye, Memlekete Özgürlük!

## Slide 15: ELECTRICAL
• Electrical Resistivity of Copper:
• Adding “impurity” atoms to Cu increases resistivity.
• Deforming Cu increases resistivity.
Adapted from Fig. 18.8, Callister & Rethwisch 8e. (Fig. 18.8 adapted from: J.O. Linde, Ann Physik 5, 219 (1932); and C.A. Wert and R.M. Thomson, Physics of Solids, 2nd edition, McGraw-Hill Company, New York, 1970.)
T (ºC)
-200
-100
0
Cu + 3.32 at%Ni
Cu + 2.16 at%Ni
deformed Cu + 1.12 at%Ni
1
2
3
4
5
6
Resistivity, r
(10-8 Ohm-m)
0
Cu + 1.12 at%Ni
“Pure” Cu
Üniversiteye, Memlekete Özgürlük!

## Slide 16: THERMAL
• Space Shuttle Tiles:
-- Silica fiber insulation
offers low heat conduction.
• Thermal Conductivity
of Copper:
-- It decreases when
you add zinc!
Adapted from
Fig. 19.4W, Callister 6e. (Courtesy of Lockheed Aerospace Ceramics Systems, Sunnyvale, CA)
(Note: "W" denotes fig. is on CD-ROM.)
Adapted from Fig. 19.4, Callister & Rethwisch 8e. (Fig. 19.4 is adapted from Metals Handbook: Properties and Selection: Nonferrous alloys and Pure Metals, Vol. 2, 9th ed., H. Baker, (Managing Editor), American Society for Metals, 1979, p. 315.)
Composition (wt% Zinc)
Thermal Conductivity
(W/m-K)
400
300
200
100
0
0
10
20
30
40
100 mm
Adapted from chapter-opening photograph, Chapter 17, Callister & Rethwisch 3e. (Courtesy of Lockheed
Missiles and Space
Company, Inc.)
Üniversiteye, Memlekete Özgürlük!

## Slide 17: DETERIORATIVE
• Stress & Saltwater...
-- causes cracks!
Adapted from chapter-opening photograph, Chapter 16, Callister & Rethwisch 3e.
(from Marine Corrosion, Causes, and Prevention, John Wiley and Sons, Inc., 1975.)
4 mm
-- material:
7150-T651 Al "alloy"
(Zn,Cu,Mg,Zr)
Adapted from Fig. 11.26, Callister & Rethwisch 8e. (Provided courtesy of G.H. Narayanan and A.G. Miller, Boeing Commercial Airplane Company.)
• Heat treatment: slows
crack speed in salt water!
Adapted from Fig. 11.20(b), R.W. Hertzberg, "Deformation and Fracture Mechanics of Engineering Materials" (4th ed.), p. 505, John Wiley and Sons, 1996. (Original source: Markus O. Speidel, Brown Boveri Co.)
“held at
160ºC for 1 hr
before testing”
increasing load
crack speed (m/s)
“as-is”
10
-10
10
-8
Alloy 7178 tested in
saturated aqueous NaCl
solution at 23ºC
Üniversiteye, Memlekete Özgürlük!

## Slide 18: MAGNETIC
• Magnetic Permeability
vs. Composition:
-- Adding 3 atomic % Si
makes Fe a better
recording medium!
Adapted from C.R. Barrett, W.D. Nix, and
A.S. Tetelman, The Principles of
Engineering Materials, Fig. 1-7(a), p. 9,
Electronically reproduced
by permission of Pearson Education, Inc.,
Upper Saddle River, New Jersey.
Fig. 20.23, Callister & Rethwisch 8e.
• Magnetic Storage:
-- Recording medium
is magnetized by
recording head.
Magnetic Field
Magnetization
Fe+3%Si
Fe
Üniversiteye, Memlekete Özgürlük!

## Slide 19: OPTICAL
• Transmittance:
-- Aluminum oxide may be transparent, translucent, or
opaque depending on the material structure.
Adapted from Fig. 1.2,
Callister & Rethwisch 8e.
(Specimen preparation,
P.A. Lessing; photo by S. Tanner.)
single crystal
polycrystal:
low porosity
polycrystal:
high porosity
Üniversiteye, Memlekete Özgürlük!

## Slide 20: Structure, Processing, & Properties
ex: hardness vs structure of steel
• Properties depend on structure
Data obtained from Figs. 10.30(a)
and 10.32 with 4 wt% C composition,
and from Fig. 11.14 and associated
discussion, Callister & Rethwisch 8e.
Micrographs adapted from (a) Fig.
10.19; (b) Fig. 9.30;(c) Fig. 10.33;
and (d) Fig. 10.21, Callister & Rethwisch 8e.
ex: structure vs cooling rate of steel
• Processing can change structure
Hardness (BHN)
Cooling Rate (ºC/s)
100
2
00
3
00
4
00
5
00
6
00
0.01
0.1
1
10
100
1000
(d)
30 mm
(c)
4 mm
(b)
30 mm
(a)
30 mm
Üniversiteye, Memlekete Özgürlük!

## Slide 21
Materials in different fields
Civil Engineering
Üniversiteye, Memlekete Özgürlük!

## Slide 22
Historical Perspective
Materials drive our society
Üniversiteye, Memlekete Özgürlük!

## Slide 23
Materials in different fields
Electrical Engineering
Üniversiteye, Memlekete Özgürlük!

## Slide 24
Materials in different fields
Aerospace Engineering
Üniversiteye, Memlekete Özgürlük!

## Slide 25: Types of Materials
Metals:
  Strong, ductile
  High thermal & electrical conductivity
  Opaque, reflective.
Polymers/plastics: Covalent bonding  sharing of e’s
  Soft, ductile, low strength, low density
  Thermal & electrical insulators
  Optically translucent or transparent.
Ceramics: ionic bonding (refractory) – compounds of metallic & non-metallic elements (oxides, carbides, nitrides, sulfides)
  Brittle, glassy, elastic
  Non-conducting (insulators)
Semiconductors, nano materials, bio materials, composites
Üniversiteye, Memlekete Özgürlük!
Notes: Metals have high thermal & electrical conductivity because valence electrons are free to roam

## Slide 26
Üniversiteye, Memlekete Özgürlük!

## Slide 27
Üniversiteye, Memlekete Özgürlük!

## Slide 28: The Materials Selection Process
1.
Pick Application
Determine required Properties
Processing: changes structure and overall shape ex: casting, sintering, vapor deposition, doping, forming, joining, annealing.
Needs, environment
Material: structure, composition.
2.
Properties
Identify candidate Material(s)
3.
Material
Identify required Processing
Cost: Ease of production, access to raw materials, access to production techniques.
Üniversiteye, Memlekete Özgürlük!

## Slide 29: Example – Hip Implant
With age or certain illnesses joints deteriorate. Particularly those with large loads (such as hip).
Adapted from Fig. 22.25, Callister 7e.
Üniversiteye, Memlekete Özgürlük!

## Slide 30: Example – Hip Implant
Requirements
  mechanical strength (many cycles)
  good lubricity
  biocompatibility
Adapted from Fig. 22.24, Callister 7e.
Üniversiteye, Memlekete Özgürlük!

## Slide 31: Example – Hip Implant
Adapted from Fig. 22.26, Callister 7e.
Üniversiteye, Memlekete Özgürlük!

## Slide 32: Hip Implant
Key problems to overcome
  fixation agent to hold acetabular cup
  cup lubrication material
  femoral stem – fixing agent (“glue”)
  must avoid any debris in cup
Femoral
Stem
Ball
Acetabular
Cup and Liner
Adapted from chapter-opening photograph, Chapter 22, Callister 7e.
Üniversiteye, Memlekete Özgürlük!

## Slide 33
Selection examples
Car hood: easy to shape, strong, good transfer, moderately cheap
Space shuttle skin: extremely stable, heat resistant, money is not an issue, low weight
Satellite wings: Extremely good thermal conductivity, low weight, money is not an issue
Üniversiteye, Memlekete Özgürlük!

## Slide 34
Advanced Materials
Materials used in "High-Tec" applications, usually designed for maximum performance, and normally expensive. Examples are titanium alloys for supersonic airplanes, magnetic alloys for computer disks, special ceramics for the heat shield of the space shuttle, etc.
Üniversiteye, Memlekete Özgürlük!

## Slide 35
Üniversiteye, Memlekete Özgürlük!

## Slide 36
Future of Materials
Design of materials having specific desired characteristics directly from our knowledge of atomic structure.
Miniaturization: “Nanostructured" materials, with microstructure that has length scales between 1 and 100 nanometers with unusual properties. Electronic components, materials for quantum computing.
Smart materials: airplane wings that adjust to the air flow conditions, buildings that stabilize themselves in earthquakes, high tem. materials...
Environment-friendly materials: biodegradable or photodegradable plastics, advances in nuclear waste processing, etc.
Learning from Nature: shells and biological hard tissue can be as strong as the most advanced laboratory-produced ceramics, mollusces produce biocompatible adhesives that we do not know how to reproduce…
Materials for lightweight batteries with high storage densities, for turbine blades that can operate at 2500C, room-temperature superconductors? chemical sensors (artificial nose) of extremely high sensitivity, cotton shirts that never require ironing
Üniversiteye, Memlekete Özgürlük!

## Slide 37: SUMMARY
• Use the right material for the job.
• Understand the relation between properties,
structure, and processing.
• Recognize new design opportunities offered
by materials selection.
Course Goals:
Üniversiteye, Memlekete Özgürlük!